## Slide 1: Marginal Integrity of Contemporary Restorative Materials
A comparative in-vitro review
Dental Materials Paper Archive · 2024
Notes: Manuscript reference DMR-545C05B36A

## Slide 2: Background
Restorative longevity is governed by the material-substrate interface.
Thermal and mechanical cycling degrades marginal adaptation over time.
Surface treatments may redistribute interfacial stress.

## Slide 3: Methods
12 x 2 x 2 mm specimens, wet-polished to 1200 grit.
10,000 thermocycles, 5-55 C, 30 s dwell.
Universal testing machine, 0.5 mm/min crosshead.
Two-way ANOVA with Tukey post-hoc.

## Slide 4: Results
Treated groups showed 5-40% improvement over control (p < 0.05).
Weibull analysis indicated reduced flaw-population variability.
No specimens failed prematurely during cycling.

## Slide 5: Discussion
Findings are consistent with a compliant interfacial interlayer.
Direct spectroscopic confirmation is outside the present scope.
Clinical evaluation would be required before practice change.

## Slide 6: Conclusions
Surface treatment improved marginal integrity in vitro.
Effect size varied by material class.
Full dataset and per-specimen tables available in the archive.